## Slide 1
Majorana fermions in
hybrid superconductor-semiconductor nanowire devices
Vincent Mourik & Kun Zuo
David van Woerkom
Sebastien Plissard, Erik Bakkers
Sergey Frolov, Leo Kouwenhoven
Quantum transport group
Delft University of Technology

## Slide 2: Majoranas in condensed matter
- quasiparticles:
- not fermions: non-Abelian statistics
- show up at the ends of a 1D p-wave superconductor:
g = c + c†
1
1
2
2
A. Yu. Kitaev; Unpaired Majorana fermions in Quantum Wires, Physics Uspekhi (2001)

## Slide 3: (Lutchyn, Sau, Das Sarma, PRL 2010, Oreg, Refael, von Oppen, PRL 2010)
Majorana recipe
- One-dimensional quantum wire
- Spin-orbit interaction
External magnetic field (orthogonal to SOI)

## Slide 4
Majorana recipe
- Add s-wave superconductivity
(μ = 0)
+ Δ
Fermi niveau

## Slide 5
EZ = D
EZ > D
Majorana
Gap is closed
Topological Superconductor
“negative gap”
Topological phase transition
EZ < D
Trivial Superconductor
“positive gap”
1
1
2
2

## Slide 6
EF
superconductor
superconductor
B
Bso

## Slide 7
Tunneling experiment
1
2
3
4
A
Tunneling into a Majorana bound state:
Resonant Andreev current!
- Zero bias peak, 2e2/h conductance
- Leads to modified QPC plateau
Wimmer et al. , NJP 2011
Law, Lee & Ng PRL 2009
Notes: 7

## Slide 8
Why InSb?
High mobility
Large spin-orbit
Large g-factor
Easy ohmic contact
InSb
InAs
stem
Plissard et al., Nano Letters (2012)
length ~ 2-3 μm
diameter 80-120 nm
InSb Zinc Blende Nanowires
Notes: In collaboration with Erik Bakkers we have developed the growth of InSb nanowires. InSb wires only grow on top of an InAs stem. We can grow reproducibly wires with lengths of several micrometers and constant diameter (~100nm).
8

## Slide 9
Majorana recipe
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
500 nm
Gate voltage (V)
5
1
2
3
4
0
Conductance (2e2/h)
0
2
1.5
1
0.5
B = 4T
van Weperen et al. Nano Letters 2013

## Slide 10
Majorana recipe
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
van Weperen et al. Nano Letters 2013
B = 4T
Mobility ~ 40,000 cm2/Vs
Mean free path ~ 300 nm
quasi-ballistic transport

## Slide 11
Majorana recipe
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
k
BSO
singlet
triplet
triplet
singlet
lso = 100-300 nm
Nadj-Perge et al. PRL 2012

## Slide 12
Majorana recipe
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
Eso
E
BSO
k

## Slide 13
Majorana recipe
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
Contact spacing
= 250 nm
InSb wire
Ti/NbTiN contact (10/100 nm)
Global backgate
Rn = 1.4 kΩ

## Slide 14
1 micron
NbTiN
Ti/Au
InSb
nanowire
NbTiN
NbTiN
?
?
?
?

## Slide 15
B (T)
I (pA)
0
2000
-2000
dV/dI (a.u.)
Supercurrents surviving to 2 Tesla.
Contact spacing = 900 nm
(Dark regions near zero bias = supercurrent)
2.0
-2.0

## Slide 16
Play with gates – make ZBP due to Josephson appear at finite field!

## Slide 17
1
2
3
4
1 μm
S
N
B
1
2
3
4
(Au-InSb-NbTiN)
B = 0
0.2
0
V (mV)
dI/dV (2e2/h)
-400
0
400
2D
N-NW-S devices

## Slide 18: Finite field zero bias peak
V (mV)
B = 0
dI/dV (2e2/h)
0.5 T
More details: V. Mourik, K. Zuo et al., Science Vol. 336 no. 6084 pp. 1003-1007

## Slide 19
V (mV)
Peak onset EZ ~ D
+D
0
250
-250
Magnetic Field (T)
0
0.5
0.9
-D
0.1
1 Tesla = 1.5 meV

## Slide 20: How would Kondo effect look?
g = 2
g = 50
V (mV)

## Slide 21
V (mV)
500
-500
0
-10
10
0
(2e2/h)
175 mT
Voltage on Gate 2 (V)
A
0.2
0.7
1
2
3
4
*
Gate dependence: under S contact

## Slide 22
dI/dV
(2e2/h)
0.25
1.25
dI/dV
(2e2/h)
0.0
1.25
V (mV)
0
V (mV)
0
200
-200
200
-200
Barrier gate (V)
-1.25
0.0
Barrier gate (V)
-1.75
-0.5
1
2
3
4
*
Gate dependence: barrier gate

## Slide 23
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
✔
✔
See Supplementary Info for scans along all 4p directions in 3D space
Majorana recipe

## Slide 24
2.5 mm
Au
Au
B
1
2
3
No robust zero bias peaks observed
One-dimensional quantum wire
Spin-orbit interaction
Superconductivity
Magnetic field
✔
✔
✔
Majorana recipe

## Slide 25
Zero bias peak (ZBP) onsets at B ~ 100 mT
Ez ~ 150 μeV, so Ez ~ Δ
ZBP remains stuck to zero bias over significant range of B (peak width 30 μeV, ΔEz ~ 0.5-1.5 meV)
ZBP persist over large gate ranges for all gates, but gate tuning is required!
ZBP vanishes when B is aligned with BSO
ZBP robust in both gate and magnetic field NOT OBSERVED in several N-NW-N devices
Persistent ZBP reproduced in four N-NW-S devices and three cryostats
Our signatures of Majoranas

## Slide 26
N1
N2
S
3 gates to tune
subbands
New experiments
1 μm
gates to define barrier/QPC/QD

## Slide 27
New experiments
Interesting questions:
Are there really 2 Majorana’s?
Is a Majorana large or small compared to the device size?
Do the Majorana’s interact?
Can they be moved by gates?
……

## Slide 28
Zero bias peak at finite field

## Slide 29
Green
Purple
peak height
~5-10% x 2e2/h
Feature is reproducible

## Slide 30: Peak splitting oscillations

## Slide 32
Prada et al. PRB 2012
Das Sarma et al. PRB 2012

## Slide 33: What’s the difference?
Gates at the edge slightly different tuned

## Slide 34
S
N1
N2
correlation in peak onset
N1-S
N2-S
0T
1T
~450 mT

## Slide 35
no splitting
splitting
 not the same single MF pair
S
N1
N2

## Slide 36
splitting
no splitting
 not the same single MF pair
different
gate setting
S
N1
N2

## Slide 37
Middle gate tunes peak splitting

## Slide 38: Change of design
N1
N2
600nm S
Half the length of the Superconducting contact
Larger overlap between two Majorana’s (stronger oscillation)
Less disorder in shorter wires (more correlation)

## Slide 39: B-field dependence
- By now ZBP’s in > 10 devices.

## Slide 40
Much cleaner DOS in the new sample!

## Slide 41
N1
N2
S
BG2
Notes: BG2 = -4.5 V for single peak and BG2 = 5V for split peaks. There is might be a jump here, but in any case the peak shape is very different for these two gate values.

## Slide 42: Observations summarized
Single side measurements (true at both sides):
Zero bias feature has been reproduced
In B, gate space: peak - splitted peak oscillations
First gate under S contact is crucial to observe this
Both sides measurements:
Peak patterns globally similar at both sides
There is no correlation at detailed level
Middle gate under S contact is capable of tuning peak (splitting)

## Slide 43: Outlook: Braiding
Alicea et al. Nature Physics 2011
Hyart et al. PRB 2013

## Slide 44: Observations summarized
Single side measurements (true at both sides):
Zero bias feature has been reproduced
In B, gate space: peak - splitted peak oscillations
First gate under S contact is crucial to observe this
Both sides measurements:
Peak patterns globally similar at both sides
There is no correlation at detailed level
Middle gate under S contact is capable of tuning peak (splitting)