EFFECT OF Fe- and Ni  ION IMPLANTATION ON  THE MAGNETORESISTANCE OF  La0.7Sr0.3MnO3 THIN FILMS

E. S. Vlakhova, d, E. Wieserb,  K. A. Nenkov a, c, d, R. Groetzschelb

aInstitute of Solid State Physics, Bulgarian Academy of Sciences, 1784 Sofia, Bulgaria,

bInstitute of Ion Beam Physics and Materials Research, Forschungzentrum Rossendorf e.V., P.O. Box 510119, D-01314 Dresden, Germany,

cInstitut für Festkörper- und Werkstofforschung Dresden,  D-01171, Dresden, Germany,

dIntern. Laboratory of High Magnetic Field and Low Temperatures, 53-529 Wroclaw, Poland

Implantation of 56Fe and  58Ni  ions with low and moderate doses is employed to create point defects and lattice disorder as well as doping by Fe or Ni in order to study their influence on the magnetoresistance of La0.7Sr0.3MnO3  thin films deposited by magnetron sputtering. Two step ion implantation was carried out to distribute the implanted species across the whole layer thickness. The total dose was divided in the relation 1 : 2.5 on the energies 120 and 350 keV  and  varied between 3.5x1013 cm-2 and 5x1015 cm-2.  RBS of He+ ions in random and channeling direction was used to detect the radiation damage. With increasing implantation dose the temperature of maximum magnetoresistance shifts to lower values. The low temperature transition from metallic conductivity to an increase of resistivity with decreasing temperature and the strong scattering of the resistance values in this range observed for medium implantation doses will be discussed in the frame of  a phase separation model. Changes of the transport properties as result of a modified  microstructure formed by recrystallization of the heavily implanted samples  will be presented,  too.

Abstract category: 2. Magnetic Films, Surfaces and Multilayers.

Type of presentation: poster

Corresponding author: E. S. Vlakhov

Address: Institute of Solid State Physics, Bulgarian Academy of Sciences, 1784 Sofia, Bulgaria

e-mail address: evlakhov@issp.bas.bg